SR station bench

This model is based on the common type of bench seen on many ex SR stations. There are a number of small variations i.e. armrest with inner curl as per kit, or without, as per photos below. In SR days they were painted middle chrome green (Precision paints ref P93) which was continued by BR until late 60’s when black was used as part of the ‘corporate image’ rebranding of BR. It is unlikely that any survived to be painted NSE red. For full details of painting specs for stations etc, see www.stationcolours.info

#### Assembly

- Clean any flash from the castings and burnish with a small brass or fibreglass brush if required. Drill the small holes in the foot of 2 leg units per seat 0.5mm

- Cut the 6 small tabs around the edges of the etched seat lath unit – do not cut each lath out individually as it then becomes very time consuming to assemble a seat

- Form etch to approximate shape (half etch strip to bottom/back) and tack 2 end leg units (the ones with the hole drilled out!) to this refining the shape as you go. The thicker lath is at the top and the castings align with the half etch strips on the etch. The last lath should be at about 45 deg. on the outer curve of the leg unit. There may be a small amount of upright protruding, but this can be trimmed off later. When happy with the alignment and the seat sits square and level fit middle leg unit and complete soldering outer units to the etched  lath unit

- Fit armrests to outer ends.

- Bend wire brace so that it fits between the holes in the outer feet and touches the top underside of the middle leg unit

- Clean off any excess solder and wash completed seat to remove any excess flux etc. Allow to dry before applying primer (i.e. Halfords aerosol).  Finally paint in the appropriate colour for your layout – see info above